## Slide 1: Excited Carrier Dynamics in Condensed Matter System
From ab initio simulation
Jin Zhao
University of Science and Technology of China

## Slide 2
Back ground
Single particle dynamics
Spin dynamics
Exciton Dynamics
Outlook

## Slide 3
Carrier Dynamics in Condensed Matter Systems
Lattice
charge
orbital
spin
Condensed matter physics: Charge, spin and orbital
Important tool: First principles calculations
Multi-dimension: energy, momentum, real space, spin, time

## Slide 4
Applications of Photoexcited Carrier Dynamics
光调制器
短寿命
光探测器
中等寿命
不同光电器件对材料载流子寿命有不同要求
发光器件
长寿命
太阳能电池各种载流子动力学行为共同决定效率

## Slide 5
Determining Factors of Carrier Dynamics
No perturbation, no relaxation :
Electron / hole
Magnetic field
Spin-orbital coupling
Electric field
Photon
Phonon
Nonradiative relaxation
Radiative relaxation
Charge transport
SOC induced spin dynamics
SOC induced spin dynamics
With perturbation：
Many-body effects:
e-e interaction
e-h interaction (exciton effects)
spin-spin interaction
Other effects:
Nuclear quantum effects
Potential energy surface of the excited state

## Slide 6
Ab initio Code for Excited Carrier Dynamics
Single Particle Dynamics
GW+rtBSE
Spin Dynamics
光催化
太阳能电池
谷电子学
光电器件
光调控自旋动力学

## Slide 7
2016
郑奇靖
2018
Hefei-NAMD
Quantum decoherence
褚维斌
赵传寓
2018
郑奇靖
Spin-orbital Coupling
2021
GW + real-time BSE
2018
褚维斌
Nuclear Quantum effects
蒋翔
now
Charge transport
Dynamics in momentum space
now
田韫哲
郑镇法
史永亮

## Slide 8
Back ground
Single particle dynamics
Spin dynamics
Exciton Dynamics
Outlook

## Slide 9
Beyond Born-Oppenheimer Approximation
Mixed Quantum-Classical approximation

## Slide 10
Fewest surface hopping

## Slide 11
Surface Hopping Combined with TDKS
Nonadiabatic coupling (NAC)
A. Akimov and O. Prezhdo: Pyxaid
Q. Zheng, X. Jiang, et. al. J. Zhao: Hefei-NAMD

## Slide 12
Nonadiabatic coupling
Electron-phonon matrix elements
charge transfer dynamics
Electron-hole recombination
Electron-phonon interaction – Nonadiabatic coupling

## Slide 13
Electron-phonon interaction - Decoherence Correction

## Slide 14
What is Photocatalysis
光解水
光还原CO2
降解污染物
…
目标：通过第一性原理计算理解光催化反应机制，提出理论设计提升反应效率

## Slide 15
Crucial Processes in Photocatalysis on Surfaces
Photo-absorption
absorption spectra （DFT, GW+BSE)
Photoexcited carrier trapping
Lifetime of photoexcited carriers
Carrier migration to surface
Carrier trapping by molecules
Photochemical reaction on the surface
Excited state reaction barrier

## Slide 16
Excited Carrier Dynamics
Crucial Processes in Photocatalysis on Surfaces
Photo-absorption
absorption spectra （DFT, GW+BSE)
Photoexcited carrier trapping
Lifetime of photoexcited carriers
Carrier migration to surface
Carrier trapping by molecules
Photochemical reaction on the surface
Excited state reaction barrier

## Slide 17
CH3OH behaves as a hole scavenger on TiO2
Henderson et.al. believes that CH3O is the hole trapper in stead of CH3OH
M. Shen and M. A. Henderson, J. Phys. Chem. Lett. 2, 2707-2710 (2011)
Hole induced dissociation of CH3OH on TiO2 observed by Bing Wang et.al.

## Slide 18
M
HD
D
Hole trapping sites
~0.2%
~20~30%
~30~50%
Average from 105 trajactories
Hole transfer to HOMO (%)
Time (fs)

## Slide 19
CH3OH as a Hole Scavenger on TiO2 Surface
W. Chu, W. A. Saidi, Q. Zheng*, Y. Xie, Z. Lan, O. V. Prezhdo, H. Petek and J. Zhao* J. Am. Chem. Soc, 138, 13740, (2016)

## Slide 20
Nuclear Quantum Effects in NAMD
Mixed Quantum-Classical approximation
Q: 如何在mixed quantum-classical approximation中考虑核量子效应
A: RPMD + NAMD
Ring-polymer molecular dynamics (RPMD)

## Slide 21
Different Adsorption Structures of CH3OH on TiO2
Dissociated CH3O (DM) behaves as hole scavenger
√
√
×
×
×
×
×
×
No H-bond network
H-bond network

## Slide 22
Nuclear Quantum effects (NQEs) on the Adsorption Structures
Quantum proton delocalization
NQEs induced proton transfer
δ > 0 no proton transfer
δ < 0 proton tranfer
H-bond network
No H-bond network

## Slide 23
Nuclear Quantum effects on the Energy Level Alignment
VBM
VBM
H-bond network
NQEs change the band alignment of MD_H system, where a H-bond network is formed.

## Slide 24
Nuclear Quantum Effects on Hole Trapping
NQEs makes MD_H behave as a hole scavenger.
√
×
×
√

## Slide 25
Collective Nuclear Quantum Motion Coupled Hole Transfer
In the H-bond network, the quantum proton motion is collective, which couples with hole trapping dynamics.

## Slide 26
Experimental Evidence by STM
Dimer formation (H-bond network) improves the photochemical reaction rate.

## Slide 27
Summary - Example I
W. Chu et al. X. Li*, J. Zhao* Sci. Adv. 8, eabo2675 (2022)

## Slide 28
Outlook - Example I
M1,M2
M3,M4
RPMD/PIMD is very expensive!
Machine Learning + PIMD/RPMD
M1
M2

## Slide 29
Outlook - Part II
基态催化：
计算反应势垒，方法非常成熟
光催化：
激发态势能面
势能面交叉
激发态载流子寿命

## Slide 30
Back ground
Single particle dynamics
Spin dynamics
Exciton Dynamics
Outlook

## Slide 31
Spin-Orbital Interaction
Spin-Spin Interaction
Spin Dynamics

## Slide 32
32
Dynamics of Photogenerated Spin Hole Current
C. Zhao, et al. and J. Zhao*, Phys. Rev. B 96, 134308 (2017)
赵传寓

## Slide 33
NAMD with SOC

## Slide 34
Choices of Representations
郑奇靖

## Slide 35
Ni金属自旋轨道耦合引发超快退磁过程
Spin down electrons will NOT flip to Spin up electrons due to SOC
They will decay to spin down electrons with lower energies.
Spin up electrons will flip to Spin down electrons due to SOC

## Slide 36
自旋轨道耦合与电声耦合
+
In Ni, e-ph coupling > SOC. The electron tends to decay through the orbitals with the same spin.

## Slide 37
Ni体系超快退磁
Z. Zheng, Q. Zheng*, J. Zhao*, Phys. Rev. B 105, 085142 (2022)

## Slide 38
Excited Electron Dynamics in Bi2Se3
TSS@±S
Back scattering between TSS@+S and TSS@-S is forbidden

## Slide 39
Backscattering Between two TSS@±S Time-Reversal Partners
≠ 0
300 K
100 K
TSS@±S
CBM
TSS@Γ
TSS@±S
TSS@+S
TSS@-S
~ 20 ps
~ 100 fs
Without phonon excitation
With phonon excitation

## Slide 40
Excited State Spin Dynamics in Bi2Se3
Spin canting occurs in ~ 50 fs

## Slide 41
Ultrafast Spin Relaxation of the Excited TSS Electron
C. Zhao, Q. Zheng*, J. Zhao*, Fundamental Research in press
Z. X. Shen* et al. Phys. Rev. Lett. 122, 167401 (2019)
N. Gedik* et al. Phys. Rev. Lett. 107, 077401 (2011)

## Slide 42
Back ground
Single particle dynamics
Spin dynamics
Exciton Dynamics
Outlook

## Slide 43
Excitons in 2D Materials
A. Chernikov et al. Phys. Rev. Lett. 113 076802 (2014)
2D materials: quantum confinement significantly reduce the dielectric screening and increase the exciton binding energy
Exciton binding energy

## Slide 44
https://www.sas.upenn.edu/~jianmint/Research/
Failure of DFT
A. Morales-Garcia et al. J. Phys. Chem. C, 121, 18862 (2017)

## Slide 45
GW + BSE to Describe the Exciton
GW: self-energy take place of exchange correlation potential
Accurate Quasi-particle energies
Bethe-Salpeter Equation (BSE): Screened Coulomb (W) and exchange (v) interaction of electron and hole
Exciton binding energy and wave function

## Slide 46
Exciton Dynamics is Important
Exciton dynamics:
Exciton relaxation
Bright-to-dark transition
Single-to-multi transition
Singlet fission
Exciton annihilation (radiative and nonradiative)
…
10,000 times of GW+BSE calculations are too expensive!

## Slide 47
Realization of GW + Real-Time BSE
BSE Hamiltonian:
Coulomb Interaction:
Exchange Interaction:
Rigid dielectric function during MD
QP energy: Rigid shift from KS energy
10,000 real-time GW + BSE – 1 GW + real-time BSE
from time-dependent Kohn-Sham basis sets
From GW

## Slide 48
TDDFT
Real-time - BSE
Single-particle
two-particle
Many-body interaction：Coulomb and exchange
Exciton-phonon interaction：real-time BSE + molecular dynamics
Spin orbital coupling：adiabatic and diabatic representation
Nonadiabatic: surface hopping
Spin orbital coupling
Realization of GW + Real-Time BSE

## Slide 49
含时激子动力学方法实现

## Slide 50
Fast Intervalley Bright Exciton Scattering in Transition Metal Dichalcogenide
K
K’
K
K’
< 5 ps
Intervalley bright exciton scattering requires the spin flip and momentum transition of both electron and hole
Puzzle：how can such intervalley bright exciton happen within several picoseconds？

## Slide 51
Test of the Dielectric Function Approximation
The dielectric function and GW QP correction almost does not change with the structure

## Slide 52
Exciton Dynamics in MoS2
~1 ps
~1 ps
~40 fs
Bright Exciton transition happens in several ps

## Slide 53
Exchange Interaction Induced Bright Exciton Scattering
Single particle dynamics：e-ph
Exciton dynamics: e-ph + W (e-h Coulomb) + v (e-h exchange) + SOC
Nonadiabatic Coupling Elements：
Bright Exciton transition is induced by e-h exchange interaction

## Slide 54
Single Particle Picture
Spin particle picture: photoexcited hole keeps in K valley

## Slide 55
Summary
X. Jiang, Q. Zheng, Z. Lan, W. A. Saidi, X. Ren and J. Zhao* Sci. Adv. , 7, eabf3759, (2021)
Xiang Jiang
蒋翔
TDDFT
Real-time - BSE
Single-particle
two-particle
Many-body interaction
Exciton-phonon interaction
Spin orbital coupling
Nonadiabatic effects

## Slide 57
Back ground
Single particle dynamics
Spin dynamics
Exciton Dynamics
Outlook

## Slide 58
What can be Done Using the GW-rtBSE NAMD Simulation
Exciton Lifetime
Hot exciton Relaxation
Exciton transition
at interface
via spin valley
bright-to-dark
…
Exciton-Phonon Interaction
Exciton-Polaron interaction
Excited state potential surface from machine learning
Photo-induced phase transition
Photocatalysis
Several thousands of exciton energies can be used for machine learning

## Slide 59
NAMD Simulation in Momentum Space

## Slide 60
Phonon Excitation

## Slide 61
Journal | Number of Publications
Sci. Adv. | 3
Nat. Commun. | 1
Phys. Rev. Lett. | 3
JACS | 2
Adv. Mater. | 1
Nano Lett. | 4
ACS NANO | 1
J. Phys. Chem. Lett. | 18
Chem. Sci. | 1
Angew Chem. | 1
Publications by Hefei-NAMD（over 80）
Hefei-NAMD的应用与推广

## Slide 62
南京理工大学陆瑞峰
大连理工大学高峻峰
电子科大周柳江

## Slide 63
Video
Hefei-NAMD使用的一些经验
https://www.koushare.com/video/videodetail/11720
Hefei-NAMD基本流程介绍
https://www.bilibili.com/video/BV1p5411c7RS
Hefei-NAMD培训
https://www.koushare.com/lives/room/341102
Website:
http://staff.ustc.edu.cn/~zqj
http://staff.ustc.edu.cn/~zhaojin
https://github.com/QijingZheng
https://github.com/WeibinChu
Developers:
Dr. Qijing Zheng (郑奇靖), zqj@ustc.edu.cn
Mr. Xiang Jiang (蒋翔), jxiang@mail.ustc.edu.cn, exciton dynamics
Dr. Weibin Chu (褚维斌), wbchu@ustc.edu.cn, CA-NAC, DISH
Dr. Chuanyu Zhao (赵传寓), zhaochuanyu@zju.edu.cn, DISH
Mr. Zhenfa Zheng (郑镇法), zzfgjs@mail.ustc.edu.cn, Dynamics in momentum space
Reference & Developers

## Slide 64
Determining Factors of Carrier Dynamics
No perturbation, no relaxation :
Electron / hole
Magnetic field
Spin-orbital coupling
Electric field
Photon
Phonon
Nonradiative relaxation
Radiative relaxation
Charge transport
SOC induced spin dynamics
Magnetic field induced spin dynamics
With perturbation：
Many-body effects:
e-e interaction
e-h interaction (exciton effects)
spin-spin interaction
Other effects:
Nuclear quantum effects
Potential energy surface of the excited state

## Slide 65
兰峥岗
华南师大
Surface hopping
任新国
中科院物理所
GW+BSE
李新征
北京大学
PIMD
谭世倞
中科大
实验
王兵
中科大
实验
Hrvoje Petek
匹兹堡大学
实验
杨金龙
中科大
讨论+支持
郑奇靖
中科大副教授
褚维斌
复旦大学青年研究员
蒋翔
UC Irvine 博后
郑镇法
博士生
史永亮
华为
张丽丽
郑州大学讲师
赵传寓
腾讯
感谢基金委、科技部、中国科大的经费支持